FABRIC SPECIFICATIONS FOR

IOWA STATE PATROL UNIFORM

TROUSERS

RAEFORD MILL’S

PROBLEND STYLE 645

WEAVE				ELASTIQUE

SHADE				437 PINK TAN FOR THE BODY OF THE TROUSER

561 BLACK FOR THE LEG STRIP

WEIGHT			16.5 oz – 17.0 oz per linear yard

FIBER CONTENT			55% DACRON POLYESTER

45% WOOL WORSTED

PLY OF YARN			2-PLY WARP AND FILLING

BREAKING STRENGTH		200 POUNDS IN THE WARP

130 POUNDS IN THE FILLING

CONSTRUCTION		122 ENDS PER INCH

85 PICKS PER INCH

FIBER LENGTH			WOOL: 3 – 3.5 INCHES AVERAGE MINIMUM

POLYESTER: 3 INCHES MINIMUM

DYE PROCEDURE		PIECE DYED

KAUMOGRAPH			BACK FACE OF FABRIC MUST BE

STAMPED WITH MILL TRADEMARK

This fabric is manufactured utilizing yarn spun on the Long Staple Fiber Length Worsted Spinning System

FABRIC SPECIFICATIONS FOR

IOWA STATE PATROL UNIFORM

SHIRTS

RAEFORD MILL’S

PROBLEND STYLE 573

WEAVE				TROPICAL

SHADE				983 BROWN FOR THE BODY OF THE SHIRT

437 PINK TAN FOR THE SHOULDER STRAP

WEIGHT			11.0 oz – 11.5 oz per linear yard

FIBER CONTENT			55% DACRON POLYESTER

45% WOOL WORSTED

PLY OF YARN			3-PLY WARP AND FILLING

BREAKING STRENGTH		105 POUNDS IN THE WARP

85 POUNDS IN THE FILLING

CONSTRUCTION		55 ENDS PER INCH

46 PICKS PER INCH

FIBER LENGTH			WOOL: 3 – 3.5 INCHES AVERAGE MINIMUM

POLYESTER: 3 INCHES MINIMUM

DYE PROCEDURE		PIECE DYED

KAUMOGRAPH			BACK FACE OF FABRIC MUST BE

STAMPED WITH MILL TRADEMARK

This fabric is manufactured utilizing yarn spun on the Long Staple Fiber Length Worsted Spinning System